Poly(dopamine) and its Related poly(catecholamines): Self-Sealing Adhesive Polymers

Haeshin Lee

Department of Chemistry, KAIST, Korea

Center for Nature-inspired Technology (CNiT)

E-mail: haeshin@kaist.ac.kr

Catecholamines are found ubiquitously in nature. Wetting-resistant, adhesive foot-pads in mussels, neurotransmitters in the brain, melanin bio-pigments in the skin and eyes, squid beaks, and insect cuticles are related examples. In materials science, catecholamines have recently attracted significant attention due to the unprecedented material-independent surface-functionalization properties found in poly(dopamine) (pDA)1 and poly(norepinephrine)2,3.

The material-independent coating properties are developed only when both catechol and amine moieties coexist in a polymeric backbone. In contrast, when the both moieties are ‘not’ covalently linked, they exhibit self-sealing properties at liquid/air interfaces. The self-sealing requires only O2 in air, and other external stimuli such as light, heat, pH, and moisture as well as internal co-factors such as catalysts are not necessary. Self-sealing conceptually mimics biological healing processes in which precursors at internal liquid are polymerized and/or crosslinked at liquid/air interfaces rather occurring at a bulk liquid. Furthermore, the newly generated material at interfaces robustly attached to existing (i.e. undamaged) one, resulting in sealing properties. As self-sealing utilizes oxygen, regeneration of the catecholamine materials occurs nearly unlimited times as long as the precursor internal solution exists, and more than 100 times of self-sealing was experimentally demonstrated. Finally, this seminar will present a hemostatic needle which results in blood vessel self-sealing exhibiting no bleeding after needle injection and withdrawal4.

- H. Lee et al. Science 2007, 318, 426

- S. Hong et al. Angew. Chemie. Int. Ed. 2013, 52, 9187-91

- S. M. Kang et al. J. Am. Chem. Soc. 2009, 131, 13224-225

- M. Shin et al. Nature Mater. 2017 (http://dx.doi.org/10.1038/nmat4758)